## Slide 1: Unit I Introduction to IC technology
Topics
MOS, PMOS, NMOS, CMOS and BiCMOS Technologies:
Oxidation
Lithography
Diffusion
Ion implantation
Metallization
Encapsulation
Probe testing
6•/3/20I1n5 tegrated Resistors and Capacitors
2

## Slide 2: Acronym of VLSI
6/3/2015
2
V -> Very
L -> Large
S -> Scale
I -> Integration

## Slide 3: Types of Field Effect Transistors (The Classification)
» JFET
MOSFET (IGFET)
n-Channel JFET p-Channel JFET
n-Channel
EMOSFET
p-Channel
EMOSFET
Enhancement MOSFET
Depletion
MOSFET
n-Channel
DMOSFET
p-Channel
DMOSFET
FET
MOSFET (Metal-Oxide Semiconductor Field-Effect Transistor)
Primary component in high-density VLSI chips such as memories and microprocessors
JFET (Junction Field-Effect Transistor)
Finds application especially in analog and RF circuit design
6/3/2015
3

## Slide 4: Metal Oxide Semiconductor(MOS)
6/3/2015
4
Advantages of FET over conventional Transistors
Unipolar device i. e. operation depends on only one type of charge carriers (h or e)
Voltage controlled Device (gate voltage controls drain current)
Very high input impedance (109-1012 )
Source and drain are interchangeable in most Low-frequency applications
Low Voltage Low Current Operation is possible (Low-power consumption)
Less Noisy as Compared to BJT
No minority carrier storage (Turn off is faster)
Very small in size, occupies very small space in ICs

## Slide 5: Switch Model of NMOS Transistor
Gate
Source (of carriers)
Drain (of carriers)
| VGS |
| VGS | < | VT |
| VGS | > | VT |
Open (off) (Gate = ‘0’)
Closed (on) (Gate = ‘1’)
Ron
6/3/2015
5

## Slide 6: Switch Model of PMOS Transistor
Gate
Source
(of carriers)
Drain
(of carriers)
GS
| V |
| VGS | > | VDD – | VT | |
| VGS | < | VDD – |VT| |
Open (off) (Gate = ‘1’)
Closed (on) (Gate = ‘0’)
Ron
6/3/2015
6

## Slide 7: MOS transistors Symbols
D
D
G
G
S
D
D
G
G
S
NMOS Enhancement
PMOS
S
NMOS Depletion
Enhancement
B
S
NMOS with
Bulk Contact
Channel
6/3/2015
7

## Slide 8: MOSFET Circuit Symbols
(g) and (i) are the most commonly used symbols in VLSI logic design.
MOS devices are symmetric.
In NMOS, n+ region at higher voltage is the drain.
In PMOS p+ region at lower voltage is the drain
6/3/2015
8

## Slide 9: The NMOS Transistor Cross Section
6/3/2015
11
n areas have been doped with donor ions (arsenic) of concentration ND - electrons are the majority carriers
majority carriers
Gate oxide
n+
Source
Drain
Bulk (Body)
p areas have been doped with acceptor ions (boron) of concentration NA - holes are the
p+ stopper
Field-Oxide
(SiO2)
n+
Polysilicon Gate
L
p substrate
W

## Slide 10: Carriers and Current
6/3/2015
12
Carriers always flow from the Source to Drain
NMOS: Free electrons move from Source to Drain.
  Current direction is from Drain to Source.
PMOS: Free holes move from Source to Drain.
  Current direction is from Source to Drain.
–

## Slide 11: The MOSFET Channel
6/3/2015
14
Under certain conditions, a thin channel can be formed right underneath the Silicon- Dioxide insulating layer, electrically connecting the Drain to the Source. The depth of the channel (and hence its resistance) can be controlled by the Gate’s voltage. The length of the channel (shown in the figures above as L) and the channel’s width W, are important design parameters.

## Slide 12: REGION OF OPERATION CASE-1 (No Gate Voltage)
6/3/2015
15
Two diodes back to back exist in series.
One diode is formed by the pn junction between the n+ drain region and the p-type substrate
Second is formed by the pn junction between the n+ source region and the p-type substrate
These diodes prevent any flow of the current.
There exist a very high resistance.

## Slide 13: NMos Cut View
6/3/2015
16

## Slide 14
6/3/2015
17

## Slide 15: REGION OF OPERATION Creating a channel
6/3/2015
18
Apply some positive voltage on the gate terminal.
This positive voltage pushes the holes downward in the substrate region.
This causes the electrons to accumulate under the gate terminal.
At the same time the positive voltage on the gate also attracts the electrons from the n+ region to accumulate under the gate terminal.

## Slide 16
6/3/2015
19

## Slide 17
6/3/2015
20

## Slide 18
6/3/2015
21

## Slide 19: REGION OF OPERATION Creating a channel
6/3/2015
22
When sufficient electrons are accumulated under the gate an n-region is created, connecting the drain and the source
This causes the current to flow from the drain to source
The channel is formed by inverting the substrate surface from p to n, thus induced channel is also called as the inversion layer.
The voltage between gate and source called vgs at which there are sufficient electron under the gate to form a conducting channel is called threshold voltage Vth.

## Slide 20: Formation of Channel
rst, the holes are
pelled by the ositive gate voltage, aving behind egative ions and rming a depletion gion. Next,
ctrons are attracted
the interface,
Fi re p le n fo re ele to
creating a channel
(“inversion layer”).
6/3/2015
23

## Slide 21: MOS Transistor Current direction
6/3/2015
24
The source terminal of an n-channel(p-channel) transistor is defined as whichever of the two terminals has a lower(higher) voltage.
When a transistor is turned ON, current flows from the drain to source in an n-channel device and from source to drain in a p-channel transistor.
In both cases, the actual carriers travel from the source to drain.
The current directions are different because n-channel carriers are negative, whereas p-channel carriers are positive.

## Slide 22: MOS I/V
6/3/2015
25
For a NMOS, a necessary
condition for the channel to exist is:
VGS
 VTH

## Slide 23: REGION OF OPERATION Applying small Vds
6/3/2015
26
Now we applying some small voltage between source and drain
The voltage Vds causes a current to flow from drain to gate.
Now as we increase the gate voltage, more current will flow.
Increasing the gate voltage above the threshold voltage enhances the channel, hence this mode is called as enhancement mode operation.

## Slide 24: Operation – nMOS Transistor
6/3/2015
27
Accumulation Mode - If Vgs < 0, then an electric field is established across the substrate.
Depletion Mode -If 0<Vgs< Vtn, the region under gate will be depleted of charges.
Inversion Mode – If Vgs > Vtn, the region below the gate will be inverted.

## Slide 25: Operation – nMOS Transistor
6/3/2015
28

## Slide 26
V =0
Operation – nMOS Transistor
6/3/2015
29

## Slide 27: Operation – nMOS Transistor
6/3/2015
30

## Slide 28: Operation – nMOS Transistor
6/3/2015
31

## Slide 29: Operation – nMOS Transistor
6/3/2015
32

## Slide 30: Operation – nMOS Transistor
6/3/2015
33

## Slide 31: Voltage-Dependent Resistor
ion channel
FET can be resistor.
charge side the
The invers of a MOS seen as a
Since the density in
channel depends on the gate voltage, this resistance is also voltage-dependent.
6/3/2015
34

## Slide 32: Channel Potential Variation
there’s a
nnel resistance ween drain and
e, and if drain is
d higher than ource, then the ntial between
“ince cha bet sourc biase the s pote
gate and channel will decrease from source to drain.
6/3/2015
35

## Slide 33: Channel Pinch-Off
tial
etween drain omes more inversion
h the
rts to pinch rain.
VGs - Vth, at drain es off, and
As the poten difference b and gate bec positive, the layer beneat interface sta off around d
When VD s> the channel totally pinch
when VD s< VGs - Vth, the channel length starts to decrease.
6/3/2015
36

## Slide 34
6/3/2015
37

## Slide 35
6/3/2015
38

## Slide 36
6/3/2015
39

## Slide 37: Transistor in Saturation Mode
S
D
G
VGS
VDS > VGS - VT
ID
VGS - VT
-
+
n+
n+
Assuming VGS > VT
6/3/2015
40
VDS
Pinch-off
B
The current remains constant (saturates).

## Slide 38: During “pinchoff”
Does this mean that the current i =0 ? Actually, it does not. A MOSFET
that is “pinched off” at the drain end of the channel still conducts current:
The large E in the depletion region surrounding the drain will sweep electrons across the end of the pinched off channel to the drain.
This is very similar to the operation of the BJT. For an npn BJT, the electric field of the reversed biased CBJ swept electrons from the base to the collector regions.
6/3/2015
41

## Slide 39: N-Channel MOSFET characteristics
6/3/2015
42

## Slide 40
6/3/2015
43

## Slide 41
6/3/2015
44

## Slide 42: Enhancement-Mode PMOS Transistors: Structure
p-type source and drain
regions in n-type substrate.
vGS < 0 required to create p- type inversion layer in channel region
For current flow, vGS < vTP
To maintain reverse bias on source-substrate and drain- substrate junctions, vSB < 0 and vDB < 0
Positive bulk-source potential causes VTP to become more negative
6/3/2015
45

## Slide 43: P-channel MOSFET characteristics
linear
6/3/2015
46
saturation
p transistor

## Slide 44: Depletion-Mode MOSFETS
NMOS transistors with
Ion implantation process is used to form a built-in n-type channel in the device to connect source and drain by a resistive channel
Non-zero drain current for vGS = 0; negative vGS required to turn device off.
VTN  0
6/3/2015
47

## Slide 45
6/3/2015
48

## Slide 46
6/3/2015
49

## Slide 47: pMOS are 2.5 time slower than nMOS due to electron and hole mobilities
6/3/2015
50

## Slide 48: nMOS fabrication steps
61
Processing is carried out on a thin wafer cut from a single crystal of silicon of high purity into which the required p-impurities are introduced as the crystal is grown.
A layer of silicon dioxide (Si02) is grown all over the surface of the wafer to protect the surface, act as a barrier to dopants during processing, and provide a generally insulating substrate on to which other layers may be deposited and patterned.
The surface is now covered with a photoresist which is deposited onto the wafer and spun to achieve an even distribution of the required thickness.
The photoresist layer is then exposed to ultraviolet light through a mask which defines those regions into which diffusion is to take place together with transistor channels.
These areas are subsequently readily etched away together with the underlying silicon dioxide so that the wafer surface is exposed in the window defined by the mask.
The remaining photoresist is removed and a thin layer of Si02 is grown over the entire chip surface and then polysilicon is deposited on top of this to form the gate structure.
Further photoresist coating and masking allows the polysilicon to be patterned (as shown in Step 6) and then the thin oxide is removed to expose areas into which
Thick oxide (Si02) is grown over all again and is then masked with photoresist and etched to expose selected areas of the polysilicon gate and the drain and source areas where connections (i.e. contact cuts) are to be made.
The whole chip then has metal (aluminium) deposited over its surface. This metal layer is then masked and etched to form the required interconnection pattern.

## Slide 49
1.
2.
3.
………………………………………
………………………………………
………………………………………
Substrate
Thick oxide (1m)
Photoresist
p
p
p
62

## Slide 50: …………………………………………
4.
5.
……………………
…………………………………………………………
……………………………………
Window in oxide
Mask
UV light
p
p
63

## Slide 51: …………………………………………………………………………… ……… …………
6.
7.
…………
………
……………………
Patterned Poly. (1-2 m)
On thin oxide
( 800-1000A0 )
…………………………………………
……
……
…………
…………
n+ diffusion (1 m deep)
p
p
64

## Slide 52
8.
……………………
………………
…………………………………………
…
…
…….…………
…………
…………
Contact holes (cuts)
……………………
…………
……………………
…………
…
…
…………
……
9.
…………
………………
…………
…………………………………………
…
…
…….…………
…………
…………
Patterned Metallization (aluminum
1 m)
……………………
…………
……………………
…………
…
…
…………
……
p
p
65

## Slide 53: CMOS FABRICATION
66
There are a number of approaches to CMOS fabrication, including the p-well, the n-well, the twin-tub, and the silicon-on-insulator processes.

## Slide 54: The p-well Process
67
In primitive terms, the structure consists of an n- type substrate in which p-devices may
be formed by suitable masking and diffusion and, in order to accommodate n-type devices,
a deep p-well is diffused into the n-type substrate as shown.

## Slide 55: The p-well CMOS fabrication
68
In all other respects-masking, patterning, and diffusion-the process is similar to
nMOS fabrication. In summary, typical processing steps are:
Mask 1 - defines the areas in which the deep p-well diffusions are to take place.
Mask 2 - defines the thinox regions, namely those areas where the thick oxide is to be stripped and thin oxide grown to accommodate p- and n-transistors and wires.
Mask 3 - used to pattern the polysilicon layer which is deposited after the thin
oxide.
Mask 4 - A p-plus mask is now used (to be in effect "Anded" with Mask 2) to define all areas where p-diffusion is to take place.
Mask 5 - This is usually performed using the negative form of the p-plus mask and defines those areas where n-type diffusion is to take place.
Mask 6 - Contact cuts are now defined.
Mask 7 - The metal layer pattern is defined by this mask.
Mask 8 - An overall passivation (overglass) layer is now applied and Mask 8 ts needed to define the openings for access to bonding pads.

## Slide 56: ………………………………………
…
1.
p-well (4-5 m)
SiO2
……
…
…
2.
Thin oxide and polysilicon
Polysilicon
p
p
n
n
69

## Slide 57
……
…
…
3.
p-diffusion
P+ mask (positive)
……
…
…
4.
n-diffusion
P+ mask (negative)
p
n
p
n
70

## Slide 58
Vin
n
p
Vout
VSS
VDD
CMOS p-well inverter showing VDD and VSS substrate connections
Polysilicon Oxide
n-diffusion P-diffusion
71

## Slide 59
Vin
p
n
Vout
VSS
VDD
CMOS n-well inverter showing VDD and VSS substrate connections
Polysilicon Oxide
n-diffusion P-diffusion
72

## Slide 60: The n-well Process
As indicated earlier, although the p-well process is widely used, n-well fabrication has also gained wide acceptance, initially as a retrofit to nMOS lines.
6/3/2015
73

## Slide 61: The twin-tub-Tub Process
6/3/2015
74
A logical extension of the p-well and n-well approaches is the twin-tub fabrication process.
Here we start with a substrate of high resistivity n-type material and then create both .. n-well and p-well regions. Through this process it is possible to preserve the performance of n-transistors without compromising the p-transistors. Doping control is more readily achieved
and some relaxation in manufacturing tolerances results.
This is particularly important as far
as latch-up is concerned.

## Slide 62
Vin
Vout
VSS
VDD
Twin-tub structure
( A logical extension of the p-well and n-well)
Polysilicon Oxide
n-diffusion P-diffusion
n substrate
n well p well
Epitaxial layer
6/3/2015
75

## Slide 63: Bi-CMOS
Bipolar compatible CMOS(Bi-CMOS) technology: Introduced in early 1980s
Combines Bipolar and CMOS logic
Low power dissipation High packing density
High speed
High output
drive
High Noise Margin
High transconductance
(gm)
High input impedance
6/3/2015
76

## Slide 64: Features
The objective of the Bi-CMOS is to combine bipolar and CMOS so as to
exploit the advantages of both the technologies.
Today Bi-CMOS has become one of the dominant technologies used for high speed, low power and highly functional VLSI circuits.
The process step required for both CMOS and bipolar are almost similar The primary approach to realize high performance Bi-CMOS devices is the
addition of bipolar process steps to a baseline CMOS process.
The Bi-CMOS gates could be used as an effective way of speeding up the VLSI circuits.
The applications of Bi-CMOS are vast.
Advantages of bipolar and CMOS circuits can be retained in Bi-CMOS chips.
B6i-/3C/20M15OS technology enables high performance integrated circuits IC’s b77ut
increases process complexity.

## Slide 65: Characteristics of Bipolar Technology
Higher switching speed
Higher current drive per unit area, higher gain
Generally better noise performance and better high frequency characteristics
Improved I/O speed (particularly significant with the growing importance
of package limitations in high speed systems).
high power dissipation
lower input impedance (high drive current)
low packing density
low delay sensitivity to load
It6/3is/20e15ssentially unidirectional.
78

## Slide 66: Characteristics of CMOS
6/3/2015
79
Lower static power dissipation
Higher noise margins Higher packing density
High yield with large integrated complex functions High input impedance (low drive current)
Scalable threshold voltage High delay load sensitivity
Low output drive current (issue when driving large capacitive loads) Bi-directional capability (drain & source are interchangeable)
A near ideal switching device, Low gain

## Slide 67: Bi-CMOS FABRICATION PROCESS
6/3/2015
80
CMOS process process
1 . N-well
step)
PMOS source and drain
NMOS source and drain
BI-POLAR
n+ sub-collector
P base doping(extra
p+ base contact
n+ emitter